## STRUCTURE AND DIMENSIONS

- Central FRP strength member Ø 1.3 mm - Peripheric elements 6 * Microbundle containing Ø 1.1/1.3 mm maximum 12 optical fibres Ø 250 µm * waterblocking element * dummies Ø1.3 mm - Reinforcing watertight aramid yarns - Outer sheath B-Lite Black Ø 5.60 mm Thickness : 0.65 mm

MECHANICAL AND THERMAL PERFORMANCES

- Weight 25 kg/km - Maximum pulling force (IEC-794-1-E1) 70 daN - Maximum operating pulling force 25 daN - Minimum bending radius without tension 70 mm - Minimum bending radius with tension 105 mm - Compression (IEC-794-1-E3) 100 daN/dm - Impacts (IEC-794-1-E4) 10 impacts of 1 N.m - Operating temperature range (IEC-794-1-F1) -20°C +60°C - Storage temperature range -30°C +60°C

MARKING AND STANDARD LENGTHS

- Marking : " NEXANS MMB-0613-xxyyy-SP935" + task number + metric marking - Standard lengths : 1070 m ± 2%, 2170 m ± 2

1 : Central FRP strength member

2 : Microbundle

3 : Optical fibres

4 : Waterblocking elements

5 : Reinforcing watertight aramid yarns

6 : Outer sheath