Page 1/2

Application Air-Blown Installation into Micro-Ducts (5,5/7mm)

Design Optical Fibres Water blocked Buffer Tube Tensile Strength Elements PE-Jacket (orange)

Features All Dielectric Cable Easy Fibre Access Light Weight - Optimised for Air-Blown Installation Version illustrated is the 4 Fibre Cable

| Fibre Count | AT-Code** |  | Sheath Marking (Inkjet) |
| --- | --- | --- | --- |
| 4 | AT-3BE7FX4-004 |  | [Meter Marking] 4 SM G.652. D VAS/PE FTTH MICRO TUBE [ID] ENERGI HORSENS BREDBÅND A/S LYSLEDERKABEL - GIV AGT - USYNLIGT LASERLYS OFS [YYYY/WW] YYYY = year of the manufacture WW = week of the manufacture |

**Please refer to the OFS AT- Code. The blanks specify the fibre type.

Cable Diameter (calc.): 	3.9 mm

Cable Weight (calc.):		14 kg/km

| Identification |
| --- |
| Fibre Colour Code: |  |  |
|  | 1 | Red |  |  |  |  |  |  |  |  |  |  |  |
|  | 2 | Green |  |  |  |  |  |  |  |  |  |  |  |
|  | 3 | Blue |  |  |  |  |  |  |  |  |  |  |  |
|  | 4 | Yellow |  |  |  |  |  |  |  |  |  |  |  |
| Mechanical Properties and Environmental Behaviour Tests according to EN 187105 and IEC 60794 |
|  | Parameter | Requirement | Value |
| Tensile Performance: | Short term load, | - No changes in attenuation | Load: 1x W |
| EN 187105-5.5.4 IEC 60794-1-2-E1A and E1B | during installation | before versus after load* | W is the weight of the cable in N |
|  |  | - Max. fibre strain 0.33% |  |
| Crush Performance: | Short term load | - No changes in attenuation | Load: 1000 N |
| EN 187105-5.5.3 IEC 60794-1-2-E3 |  | before versus after load* |  |
|  |  | - No damage** |  |
| Bending Performance: | Handling fixed installed | - No attenuation increase* | Bend radius: 90 mm |
| EN 187105-5.5.1 IEC 60794-1-2-E11 | During installation | - No changes in attenuation | Bend radius: 120 mm |
|  | (under load) | before versus after load* |  |
| Temperatures: | Operation | - No attenuation increase* | -30 to +70°C |
| EN 187105-5.6.1 IEC 60794-1-2-F1 | Installation |  | - 5 to +40°C |
|  | Storage/Shipping |  | -40 to +70°C |
| * ** | No changes in attenuation means that any changes in measurement value, either positive or negative within the uncertainty of measurement shall be ignored. The total uncertainty of measurement shall be less than of equal to 0.05 dB. Mechanical damage – when examined visually without magnification, there shall be no evidence of damage to the sheath. The imprint of plates will not be considered as damage. |
| The information is believed to be accurate at time of issue. OFS reserves the right to improve, enhance and modify the features and specifications of OFS products without prior notification. Please ensure you have the latest version of the data sheet. This data sheet is property of OFS. | For additional information please contact your sales representative. You can also visit our website at http://www.ofsoptics.com. Telephone: +49 (0) 228 7489 201 Email: saleseurope@ofsoptics.com |

Page 2/2