Cable Cross-section

# Text boxes

## Optical and mechanical characteristics of a standard single mode fiber

Mode field diameter (1310 nm) :	9.2 micron ( 0.4 micron

Mode field diameter (1550 nm) :	10.5 micron ( 1.0 micron

Cladding diameter :	125 micron ( 1.0 micron

Mode field concentricity error:	( 0.8 micron

Cladding non circularity :	( 1 %

Refractive index profile :	step

Design :	matched cladding

Effective group index of refraction Neff (at 1310nm):	1.4675

Effective group index of refraction Neff (at 1550nm):	1.4681

Numerical aperture	0.13

Cut off wavelength of cabled fiber :	( 1250 nm

Attenuation at 1310 nm :	( 0.35  dB/km

Attenuation at 1550 nm :	( 0.24  dB/km

Dispersion in the range 1288 to 1339 nm :	( 3.5 ps/nm x km

Dispersion at 1550 nm :	( 18 ps/nm x km